Technical Data Sheet (TDS)

# Product Name: Polypropylene Insulation Support Netting

# Product Description:

A lightweight biaxially oriented polypropylene (BOPP) mesh netting designed to support insulation materials (e.g. glass or mineral wool) in non-habitable areas such as lofts, rafters, and subfloors.

| Material | Polypropylene (PP) |
| --- | --- |
| Mesh Type | Biaxially oriented, quadrangular |
| Colour | Black |
| UV Resistance | Yes |
| Flame Retardancy | Not fire-rated |
| Application Method | Staple or tack to timber joists or rafters |
| Intended Use | Support insulation in non-visible, non-habitable internal areas |

| DIMENSIONAL | TEST | UNIT | VALUE | TOL. | NOTES |
| --- | --- | --- | --- | --- | --- |
| CHARACTERISTICS | METHOD |  |  |  |  |
| Unit weight | ISO 9864 | g/m² | 15 | ± 10% | a |
| Mesh size |  | mm | 20 x 20 (MD x TD) |  | a, c |
| Net width |  | m | 1,00-2,00 | -2% + 3% | a |
| Roll length |  | m | 100 | -2% + 3% | a |
| MECHANICAL | TEST | UNIT | VALUE | TOL. | NOTES |
| CHARACTERISTICS | METHOD |  |  |  |  |
| MD tensile strength | ISO 10319 | kN/m | 1.045 | ± 10% | c |
| MD elongation at break | ISO 10319 | % | 18.95 |  | a, c |
| TD tensile strength | ISO 10319 | kN/m | 0,715 | ± 10% | c |
| TD elongation at break | ISO 10319 | % | 27.45 |  | a, c |
| NOTES: |  |  |  |  |  |

- Nominal value (other lengths on request)

- The durability depends on actual UV irradiation. The use of agrochemicals, pesticides, fungicides containing metal salts, halogenated, acidic and sulfur substances, may affect and reduce the product durability and invalidate the guarantee

- MD = Machine Direction (Longitudinal) TD = Transversal Direction

## Compliance Statement:

- This product is not covered by a designated standard under the UK Construction Products Regulation (CPR) and therefore does      not require UKCA or CE marking.

- It is not fire-rated and is not intended for use in fire-sensitive or habitable areas.

- No specific British Standards are applicable for this category or use case.

## Safety and Handling:

- Ensure the product is not exposed to open flame or excessive heat.

- Do not use as a structural support or finished surface layer.

- Install in line with typical construction practices for insulation support